## Slide 1: UHV Techniques
Dr. Luca Artiglia Paul Scherrer Institut
luca.artiglia@psi.ch
As part of the course ‘Molecular Aspects of Catalysts and Surfaces‘
529-0611-00L

## Slide 2
What is Vacuum?
The term VACUUM can be used to describe these conditions:
1) Complete absence of matter (definite volume in which gases are almost absent – e.g. interstellar space)
2) Physical state in which the pressure in a definite volume is smaller than in the surroundings (e.g. smaller than the atmospheric pressure)
An example: ρgas = 2·1019 mol/cm3 (atmospheric pressure)
ρgas = 109 mol/cm3 (orbiting satellite)

## Slide 3
Some applications of Vacuum
Reduce the concentration of a gas below a critical level (e.g. O2 in bulbs)
Avoid gas-driven physico-chemical processes (e.g. experiments studying the gas-surface interaction) and increase the mean free path of particles (e.g. ion and electron spectroscopies)
Thermal insulation
Degasification of liquids

## Slide 4
Vacuum | Pressure (torr) | Number Density (m-3) | M.F.P. (m) | Surface Collision Freq. (m-2·s-1) | Monolayer Formation Time (s)
Atmosphere | 760 | 2.71025 | 7108 | 31027 | 3.310-9
Rough | 10-1-103 | 3.51019 | 0.05 | 41021 | 2.510-3
High | 10-3-106 | 3.51016 | 50 | 41018 | 2.5
Very high | 10-6-109 | 3.51013 | 50103 | 41015 | 2.5103
Ultrahigh | 10-9-1012 | 3.51010 | 50106 | 41012 | 2.5106 (29 days!)
Vacuum classification

## Slide 5
Gas flow regimes
The mean free path is the average distance that a gas molecule can travel before colliding with another molecule and is determined by:
- Size of molecule (2r)
- Pressure (p)
- Temperature (T)
a =
k
T
(2r)2 p
 2
.

## Slide 6
The gas in a vacuum system can be in a viscous state, in a molecular state (or in a transition state) depending on the dimensionless parameter know as the Knudsen number (Kn) that is the ratio between the mean free path and the characteristic dimension of the flow channel.
Viscous Flow
(momentum transfer
between molecules)
Molecular Flow
(molecules move
independently)
P> 1 mbar
P<10-3 mbar

## Slide 7
Creation of Vacuum: pumping technology
1) Primary pumping systems: mechanical pumps that decrease the pressure from atmospheric pressure pressures close to the ultra-high vacuum (10-6-10-8 mbar)
- Rough pumps (atmospheric pressure down to 10-3 mbar): membrane pumps, rotary pumps, scroll pumps, roots pumps
- Turbomolecular Pumps (from the mbar to about 10-9 mbar )
2) UHV pumping systems: pumps that work at low pressure and, thanks to their efficiency, allow reaching/improving the ultra-high vacuum (10-6-10-11 mbar).
- Ion Pumps (from 10-6 mbar to 10-11 mbar)
- Getter Pump
- Titanium Sublimation Pump

## Slide 8
Rough pumps: membrane and rotary pumps
Membrane
Combined movement of a diaphragm (plastic-rubber) and suitable valves (check, butterfly, flap valves)
Volume increased = fluid drawn into the chamber
Volume decreased = fluid forced out
Dry pumps
Can handle gas and liquids
The flow rate depends on the diaphragm diameter and its stroke length
Ultimate vacuum is in the mbar (larger pumps can reach 10-1 mbar)
Rotary
Consists of vanes mounted to an eccentric rotor. The vanes rotate inside a cavity
Vanes are sealed on all edges. The rotation generates a volume expansion (gas pumping)-reduction (exhaust release)
Oil pumps: oil and gas are mixed inside the pump and separated externally
Multiple stage pump can generate a good vacuum (down to 10-3 mbar)
Low efficiency but possibility to pump gas, gas + dust and water

## Slide 9
Rough pumps: scroll and roots pumps
Scroll
One of the scrolls is fixed, while the other orbits eccentrically without rotating. Compressing pockets of fluid form between the scrolls and are driven to the exhaust port
Dry pumps
High efficiency
Small gas pulsation, less vibrations
Difficult maintenance
Ultimate vacuum is in the 10-2 mbar range
Two 8-shaped synchronously counter-rotating rotors rotate contactlessly ( small gap) in a housing
Dry pumps
Can generate a good vacuum (low 10-2 mbar)
No friction in the suction chamber, operation at high speed, large flow rate
Roots

## Slide 10
Turbomolecular pumps
A turbomolecular pump is used to obtain and maintain high vacuum.
These pumps work on the principle that gas molecules can be given momentum in a desired direction by repeated collision with a moving solid surface.
A rapidly spinning fan rotor (50000-100000 rpm) 'hits' gas molecules from the inlet of the pump towards the exhaust in order to create or maintain vacuum.

## Slide 11
Ion pumps
An ion pump is a static pump capable of reaching pressures as low as 10−11 mbar
Can be turned on only at pressures around (or less than) 10-4 mbar
A strong electrical voltage (typically 3–7 kV) is applied to the anode, producing free electrons. Electrons get caught by the magnetic field and rotate around it
Electrons hit gas molecules ionizing them
Positively charged molecules accelerates toward the cathode (grounded) at high velocity
The cathode is sputtered and titanium compounds deposit on the anode
The cathode acts as a getter (e.g. adsorbs inert gases)

## Slide 12
Static pumps
Non-evaporable getter
Static pumps helping to establish and maintain ultra-high vacuum
Porous alloys or powder mixtures of Al, Zr, Ti, V and Fe, forming stable compounds with active gases
Can be placed in narrow/difficult to reach spaces (particle accelerators)
Activated by annealing to >550 K
Static pump helping to refine the vacuum
Titanium filament through which a high current (typically around 40 A) is passed periodically
Titanium sublimates and coats the surrounding chamber walls
Components of the residual gas in the chamber which collide with the chamber wall react with titanium to form stable, solid products
Titanium sublimation

## Slide 13
Vacuum measurement
Low vacuum: Pirani (atm. pressure – 10-4 mbar)
Two Pt filaments are the arms of a Wheatstone bridge and heated to a constant temperature
Residual gases conduct away part of the thermal energy of the measurement filament. The amount of electrical current needed to restore its temperature is converted to a pressure readout
High vacuum: cold cathode (10-4-10-9 mbar)
2 electrodes: anode, cathode + permanent magnetic field (works like a ion pump!)
The pressure is measured through a gas discharge in the gauge head. The gas discharge is obtained by applying a high voltage
High-Ultrahigh vacuum: hot cathode (10-4-10-11 mbar)
3 electrodes: filament, collector, grid
The filament emits electrons, which are attracted to a polarized grid
Residual gas molecules are ionized by the electrons and attracted by the collector. Pressure reading is determined by the electronics from the collector current.

## Slide 14
TPD
Temperature Programmed Desorption

## Slide 15
Temperature programmed desorption*
Ultra high vacuum can be used to study the adsorption/reaction of molecules on a surface (monolayer formation time in UHV 103-106 s). Discussion based on Langmuir ad-(de-)sorption isotherm
Langmuir Adsorption-Desorption
Adsorption is localized (adsorbed particles are immobile)
Substrate surface is saturated at Θ = 1 ML (all adsorption sites occupied)
No interactions between the adsorbed particles
Kinetics
νn: Pre-exponential factor
n: Desorption order
Θ: Surface coverage
Edes: Activation energy for desorption
If k (rate constant) is described by an Arrhenius eq.:
The rate law is then referred to as the Polanyi-Wigner equation:
*Resource for further reading: Temperature-Programmed Desorption (TPD). Thermal Desorption Spectroscopy (TDS), Sven L.M. Schroeder and Michael Gottfried, June 2002, available online.

## Slide 16
Temperature programmed desorption
A typical TPD experiment (UHV):
Clean sample surface exposed to a precise amount of gas (usually measured in Langmuirs – 1 L = 10−6 Torr · s)
Sample placed in front of a quadrupole mass spectrometer (QMS) and heated with a precise rate (β)
The quadrupole acts as a filter, separating ions with different m/z, which are then collected
A typical spectrum shows the intensity of a specific m/z vs. temperature

## Slide 17
Temperature programmed desorption
If the pumping rate is faster than the desorption rate (no readsorption) a series of separated peaks can be recorded (each of them corresponding to a surface desorption process)
A TPD experiment can give important information:
Heat of desorption
Surface coverage (quantification of the monolayer)
Surface reactivity (gas-substrate interaction, adsorption sites)
Kinetics of desorption
Initial increase is mainly determined by Edes
Pressure drop gives information about the order of the desorption process
~Θn
~
Tm

## Slide 18
Temperature programmed desorption
Spectral interpretation is most commonly performed using the Polanyi-Wigner equation
In a TPD experiment β is the heating rate, defined as β = dT/dt = const. Thus dt = dT/β can be substituted in the equation to give
When T = Tmax
This equation can be used to obtain ΔEdes from TPD spectra (see the next slides)

## Slide 19
Spectra obtained at different Θ
First order kinetics (molecular)
The desorption peak areas depend on Θ
The desorption peaks are asymmetric
Tm constant with increasing Θ
Tm increases with ΔEdes

## Slide 20
.
First order kinetics: approximate evaluation of ΔEdes
*P. A. Redhead, Vacuum 12, 203-211 (1962).
In 1962 Redhead, assuming that activation parameters are independent of surface coverage and that desorption followed 1st order kinetics, derived a simple equation.*
Solving this equation for ΔEdes gives:
The second part in the brackets is small relative to the first, and can be approximated to 3.64 (error is less than 1.5% for 108 < ν/β < 1013 K-1)
Tm and β are determined experimentally
The activation energy from a single desorption spectrum can be estimated using an approximate value for ν. ν = 1013 s-1 is a commonly chosen value.
As an example: in this case Tm= 117 K.
Assuming ν=1.0·1013 s-1 and β=2 K/s
ΔEdes= 29.5 kJ/mol
Tm

## Slide 21
.
First order kinetics: approximate evaluation of ΔEdes from curves having different β
A series of spectra for the same Θ is acquired employing different β = dT/dt = const. From each spectrum, the temperature of the desorption rate maximum Tm is determined
Taking the ln and rearranging..
Plotting of ln(T2m/β) vs. 1/Tm for a series of β values provides ΔEdes from the slope and ν from the intercept with the ordinate

## Slide 22
.
Second order kinetics (recombinative desoprtion)
Spectra obtained at different Θ
Tm shifts with increasing Θ
Characteristic nearly symmetric peak shape with respect to Tm
Θ(Tm) is a half of the value before desorption
dividing by the units and rearranging we obtain:
Plotting the ln(T2m/β) vs. 1/Tm for a series of β values provides ΔEdes from the slope and (if Θ is known) ν from the intercept with the ordinate

## Slide 23
.
Leading edge analysis
*E. Habenschaden, J. Küppers, Surf. Sci. 138, L147 (1984).
But the activation parameters often depend on the coverage and temperature!
Habenschaden and Küppers leading edge method*
Leading edge: Θ almost unchanged
The rate of desorption is evaluated from each single leading edge
ln(rdes) plotted vs. 1/T. The slope gives ΔEdes and the intercept with y gives ν
Leading edge
Increasing Θ, Tm shifts negatively due adsorbate-adsorbate interactions

## Slide 24
An example of TPD applied to the study of a catalytic reaction

## Slide 25
Carbon monoxide oxidation on a Pt foil

## Slide 26
CO and O2 desorption
Procedure: 50 L of gas dosed on the clean foil at RT. Sample heated from RT to 700°C with β=10 K/s
Molecular adsorption (first order)
Two main desorption peaks (a foil is polycristalline) at ca. 110 and 225°C
Dissociative adsorption (recombinative desorption process)
Multiple desorption peaks at higher temperature than for CO (larger ΔEdes)

## Slide 27
Temperature programmed reaction (TPR)
Procedure: 50 L of CO dosed on the clean foil at RT. Sample heated from RT to 700°C with β=10 K/s while flowing 3·10-7 Torr of O2.
Sample surface saturated with CO
CO desorption peaks intensity decreases
As the CO starts to desorb, the partial pressure of O2 decreases and the signal of CO2 increases
Procedure: 50 L of O2 dosed on the clean foil at RT. Sample heated from RT to 700°C with β=10 K/s while flowing 3·10-8 Torr of CO.
Sample surface saturated with O2
CO2 is produced immediately, but its signal goes down above 300°C
CO2 production correlated with CO desorption

## Slide 28
In case of E-R mechanism the reaction should start immediately after introducing one of the reagents (in the presence of the other adsorbed)
In both TPR experiment CO2 production correlates with the presence of both reagents on the sample surface
TPR performed after CO pre-adsorption clearly demonstrates competition between the reagents for the adsorption sites (especially reaction at high temperature). CO is blocking the adsorption sites (poisoning effect), and some energy (temperature) is required to remove part of it and allow oxygen to adsorb and split
TPR performed after O2 pre-adsorption clearly demonstrates that adsorbed CO is necessary for CO2 formation (no more CO2 formed above 300°C
These model experiments support the hypothesis that a L-H mechanism operates, in good agreement with the literature

## Slide 29
XPS
X-ray Photoelectron Spectroscopy
Resource for further reading: Surface Analysis by Auger and X-ray Photoelectron Spectroscopy, D. Briggs, J.T. Grant, eds., IM Publications and SurfaceSpectra Ltd., 2003
Photoelectron Spectroscopy, Principles and Applications, S. Hüfner, eds. Springer-Verlag Berlin Heidelberg 1995,1996,2003.

## Slide 30
What is XPS?
The binding energies are characteristic of specific electron orbitals in specific atoms
XPS lines are identified by the shell from which the electron is emitted
Photoelectrons can escape only a few nm (this depends on their KE)
Nobel prize (physics) 1981
Binding energy!
Surface sensitive!
Nobel prize (physics) 1921
Photoelectric Effect
Albert Einstein

## Slide 31: XPS in a nut-shell
X-ray photoelectron spectroscopy (XPS) is a classical method for the semiquantitative analysis of surface composition
It is also referred to as Electron Spectroscopy for Chemical Analysis (ESCA)
It is based on the photoelectric effect, i.e., emission of electron following excitation of core level electrons by photons
It is surface sensitive because of the low inelastic mean free path of electrons
An XPS setup consists of a X-ray source, a sample chamber and an electron analyzer
XPS requires a source of X-rays, i.e., either from a lab-based anode or from a synchrotron
Traditionally, XPS works only in ultrahigh vacuum because of scattering of electrons in gases
XPS can also be performed in the mbar pressure range

## Slide 32: This is a lab based XPS instrument

## Slide 33: Electron energy analyzer
The most often used type of electron kinetic energy analyzers is composed of an electrostatic lens and a hemispherical analyzer
Electrostatic lens decelerates electrons to a fixed (pass) energy in the range of a few to 100 eV and at the same time focusses them on an entrance slit of the hemispheric analyzer
Electrons travel between two concentric hemispheres with a constant potential difference and reach a detector with one dimension aligning a small kinetic energy range
A spectrum is obtained by sweeping the lens electric field to cover specific kinetic energy ranges of the photoelectrons
Operation of an electron analyzer requires high vacuum to avoid scattering losses of electrons and to protect the detector

## Slide 34: The photoemission process
Photoelectron
Φ
Valence band
Core levels
Core hole
Photon
Kinetic energy
Binding energy
KE = hν – BE – Φ for a solid
KE = hν – IP for a gas
Φ : photoelectric workfunction
EF
EV

## Slide 35: Fate of core hole
Photoemission
Relaxation
Auger electron emission
or
X-ray fluorescence

## Slide 36: Why is XPS surface sensitive? XPS probe depth
X-ray photons can penetrate μm but…
Only photoelectrons from the first layers can escape without energy loss
Inelastic mean free path (λ) and probing depth strongly depends on the kinetic (and thus photon) energy
Depth profiles can be obtained either by varying the incident photon energy (tunable x-ray source) or by varying the detection angle (θ)
Contribution to the photoelectron signal from atoms below the surface decreases exponentially
In normal emission 95% of the signal comes from a 3λ depth
X-ray
e–
Ekin = hν-BE-φ
Ekin = hν-BE-φ-Δ
Contribution of atom in depth d to PE peak:
d
Θ

## Slide 37: Electron inelastic mean free path

## Slide 38: Inelastic background
X-ray
e–
Ekin = hν-BE-φ
Ekin = hν-BE-φ-Δ
d
Θ
Photoelectrons from deeper layers lose part of their energy (inelastic collisions) and are emitted with reduced KE (> BE)
XPS spectra show characteristic "stepped" background (intensity of background towards higher BE of photoemission peak is always larger than towards lower BE)
3d
3s
2p
2s
1000 Binding energy (eV) 0
0 Kinetic energy (eV) 1000

## Slide 39: A photoelectron spectrum in more detail
Peak shape
Spin-orbit splitting
Background shape
Auger peaks
Ti 2s
Shake-up
O 1s
Ti 2p1/2
Ti 2p3/2
Ti LMM
Ti L2,3M2,3V
C 1s
O KLL
Ti 3s
Ti 3p
O 2s
VB
TiO2 Survey
hv=730 eV
Binding energy scale (eV)
Auger peaks

## Slide 40: Spin-orbit splitting
n: principal quantum number l: orbital angular momentum quantum number s: spin angular momentum quantum number j =|l ± s|: total angular momentum quantum number
For l = 0, s levels are singlets, no splitting
For l > 0, p,d,f levels give rise to doublets. The spin angular momentum of electrons left in an orbital couple with the angular momentum vector
The degeneracy 2j + 1 determines the possibility for parallel and anti-parallel pairing
The ratio between the degeneracies (R), (2j++1)/(2j-+1), determines the relative peak ratio of the two peak components.
ΔE between two components = spin orbit splitting.
Magnitude of spin-orbit splitting increases with Z and decreases with distance from nucleus (same energy level, ΔE increases with decreasing l)
2p3/2
j = l - s
j = l + s
l = 0 .. s 1 .. p 2 .. d 3 .. f
n
Notes: Spin orbit splitting increases with atomic number

## Slide 41: Core level chemical shifts
Position of orbitals in atom is sensitive to its chemical environment
Chemical shift correlated with overall charge on atom (more positive charge = increased BE)
  number of substituents
  substituent electronegativity
  formal oxidation state (depending upon ionicity/covalency of bonding)
Chemical shift analysis is powerful tool for chemical composition, functional group and oxidation state analysis
Citric acid

## Slide 42: Secondary structure of a spectrum
Shake-up. An electron of the VB can be excited. The energy of this excitation will be deducted from the kinetic energy of the photoelectron. Relevant in metals, in which the valence and conduction bands overlap, empty states are available at very low excitation energies
Simultaneous excitation of a specific wave mode in the sample (e.g. surface plasmons). The kinetic energy loss is hωs (ωs is the plasmon frequence), and will repeat at multiples of ωs
Interaction of the photoemitted electron (along its trajectory) and the remaining electrons: final state effects (satellite peaks)

## Slide 43: Secondary structure of a spectrum
Multiplet splitting. Arises when an atom contains unpaired electrons (e.g. Cr3+, 3p63d3). During the photoemission process, there can be coupling between the unpaired electron in the core with the unpaired electrons in the outer shell. This can create a number of final states, which will be seen in the photoelectron spectrum as a multi-peak envelope. This creates different final states, depending on the orientation of the spin of the unpaired electrons
Cr 2p3/2

## Slide 44: Estimate of the signal intensity
Analyzer transmission
Angular acceptance
Attenuation from depth d at detection angle θ
Subshell ionization cross section
Photon flux
Contribution of element A at depth d to photoemission signal
Cross section - σ(KE) - is the probability to have the photoemission event
1015 atoms cm-2 (equivalent to a monolayer) lead to about 10-3 photoelectrons per incident photon
Typical photon flux: 1012 s-1, leads to about 109 photoelectrons s-1
Concentration of element A at depth d

## Slide 45: Ambient pressure x-ray photoelectron spectroscopy
But…XPS is historically bound to high – ultra-high vacuum
Pressure gap
Material gap
APXPS has partially filled the gaps!*
XPS up to 5 mbar (soft x-rays)
and 50 mbar (tender x-rays)
Possibility to investigate “real” samples (powders, semiconductors)
*O. Karslıoğlu, H. Bluhm, in Operando Research in Heterogeneous Catalysis, Vol. 114, Springer Series in Chemical Physics pp 31-57.

## Slide 46: Depth profile
If a tunable X-ray source (from a synchrotron) is available, a given electronic level can be excited with varying photon energies, resulting in varying photoelectron kinetic energies. Since the IMFP monotonously increases with increasing kinetic energy above about 100 eV, XPS can be used to obtain depth profiles of elements or their chemical state.
Oxidation of Au exposing a gold foil (T=373 K) to 0.3 mbar O3 (1%) in O2
New component in the Au 4f spectrum, associated with cationic gold
The appearance of a O 1s peak confirms that a Au-O bond forms
Auδ+ intensity is maximum at hν=175 eV, and decreases with increasing excitation energy (surface cationic gold)
Au0
Auδ+

## Slide 47: Depth profile
The Auδ+/Au0 ratio can be plotted vs. kinetic energy (IMFP)
It decreases demonstrating that the oxide stays at the surface
The experimental data can be fitted with a function reproducing the attenuation of the photoemission signal either in a uniform oxide layer (thickness t – straight line) or in patches of oxide overlayer (dashed line) supported on a semi-infinite metallic support
t=0.3 nm suggests that a O-Au-O trilayer forms at the surface

## Slide 48: The solid-gas interface @ NAPP (SLS-PSI)
Flow tube configuration
Heated sample holder. Sample powder pressed, dispersed in ethanol and drop-casted on a gold foil
Fast heating (e.g. from RT to stable 300°C in a few seconds)
Static chamber @ NAPP*
*F. Orlando, et al. Top. Catal. 2016, 59, 591.

## Slide 49: Carbon monoxide oxidation on Pt/CeO2
Page 49
Metal NPs (Pt, Pd, Au) supported on reducible oxides showed the best performance in the low temperature oxidation of carbon monoxide*
For CeO2: adsorption and activation of oxygen preferentially occur on the support, whereas carbon monoxide is adsorbed and supplied by the metal#
* I. X. Green, et al., Science 2011, 333, 736. M. Cargnello, et al., Science 2013, 341, 771. J. Saavedra, et al., Science 2014, 345, 1599.
Under catalytically relevant conditions: rapid reoxidation of ceria.
Ce3+ generated in the catalytic cycle is difficult too short lived to be detected under steady state conditions.
Studies employing time-resolved techniques are required to gather more information about the evolution of the active sites and their role in the reaction mechanism
# R. Kopelent, et al., Angew. Chem. Int. Ed. 2015, 54, 8728.

## Slide 50
Time-resolved RXES of Pt(1.5%)/CeO2 (ca. 1.2 nm diameter Pt NPs on powdered ceria) – oxygen excess (1%CO, 4% O2)*. Pulsed experiment: from CO+O2 to CO+inert
The Ce3+ concentration increases, thus oxygen from ceria participates in the oxidation of carbon monoxide.
The initial rate of ceria oxidation is >10 times higher than that of reduction. Active Ce3+ is short lived
Presence of spectator Ce3+ (not involved in the catalytic process) – probably formed during pretreatment of catalyst.
* R. Kopelent, et al., Angew. Chem. Int. Ed. 2015, 54, 8728.
OPEN ISSUES
What is the effect of the activation in hydrogen?
Are the active sites located at the metal/oxide interface? Exploit the surface sensitivity of XPS.
Carbon monoxide oxidation on Pt/CeO2

## Slide 51: Carbon monoxide oxidation on Pt/CeO2: experimental results
Pressure in the flow tube stabilized (root pump) at 1.0 mbar
Switch on/off the oxygen while acquiring (CO:O2 = 1:4)
Oxygen replaced by nitrogen, same pressure and stable m/z signals in ca. 10-15 seconds
To root pump
Gas line
Flow tube

## Slide 52
Activation of the sample in hydrogen (150°C, 1 hour, p=1.0 mbar)*
Ce 3d acquired from 2.2 to 5.0 keV photon energy range
*L. Artiglia, et al. J. Phys. Chem. Lett. 2017, 8, 102.
Carbon monoxide oxidation on Pt/CeO2: experimental results

## Slide 53: Carbon monoxide oxidation on Pt/CeO2: experimental results
Activation of the sample in hydrogen (150°C, 1 hour, p=1.0 mbar)
Ce 3d acquired from 2.2 to 5.0 keV photon energy range
The peaks can be separated into 5 d doublets#, associated to different final state configurations:
v0 and vI are associated to Ce3+.
v, vII and vIII are associated to Ce4+.
#P. Burroughs, et al. J. Chem. Soc., Dalton Trans. 1976, 17, 1686-1698.
*L. Artiglia, et al. J. Phys. Chem. Lett. 2017, 8, 102.
Notes: v0 and vI are associated to 3d94f2 O 2p5 and Ce 3d94f1 O 2p6 (Ce3+).
v, vII and vIII are associated to Ce 3d94f2 O 2p4, Ce 3d94f1 O 2p5 (shake-down/energy gain states) and 3d94f0 O 2p6 (Ce4+)

## Slide 54: Carbon monoxide oxidation on Pt/CeO2: experimental results
Enhancement of the Ce3+/Ce4+ ratio at low photon energy
Higher concentration of Ce3+ sites is found at the surface*
* S. Kato, Phys.Chem.Chem.Phys., 2015, 17, 5078.
On Pt free ceria (red dot) small amount of Ce3+ detected only at 2.2.kev
Simple model (exp. distribution) used to fit the experimental data and quantify the depth of reduction of ceria on Pt/CeO2:#
# A. Cimino, et al. J. Electron Spectrosc. Relat. Phenom. 1999, 104, 1.
t = 1.0 nm: Ce3+ sites are located in the outer layers of the ceria support, oxygen does not diffuse from the bulk to the surface.

## Slide 55: Carbon monoxide oxidation on Pt/CeO2: experimental results
Fast scans (1 scan ̴ 20’’) of the Ce 3d5/2 at hν=2200 eV acquired immediately after switching from CO/O2 to CO/N2
The 3d5/2 peak shape modifies between 80 and 160 seconds

## Slide 56: Carbon monoxide oxidation on Pt/CeO2: experimental results
The Ce3+/Ce4+ ratio increases significantly between 80 and 160 seconds (2200 eV)
Same experiment at 3000 eV shows only weak positive oscillations
Catalytically involved Ce3+ is at the surface
A constant background of Ce3+ is visible throughout the experiment
Spectator sites: formed after the activation, do not participate in the activation of oxygen